## Slide 1
Mn3p
24.77% Mn4+
70.02 % Mn3+
3.21% Mn2+
No | Name | Position (eV) | FWHM (eV) | Line shape | At%
1 | Mn4+-Peak 1 | 49.58 | 1.55 | GL(20) | 17.50
2 | Mn4+-Peak 2 | 50.93 | 1.55 | GL(20) | 4.52
3 | Mn4+-Peak 3 | 52.32 | 1.55 | GL(20) | 1.66
4 | Mn4+-Peak 4 | 53.72 | 1.55 | GL(20) | 0.91
5 | Mn4+-Peak 5 | 55.2 | 1.55 | GL(20) | 0.18
6 | Mn3+-Peak 1 | 48.38 | 1.4 | GL(20) | 40.99
7 | Mn3+-Peak 2 | 49.56 | 1.4 | GL(20) | 17.46
8 | Mn3+-Peak 3 | 50.75 | 1.4 | GL(20) | 9.55
9 | Mn3+-Peak 4 | 52.16 | 1.4 | GL(20) | 3.98
10 | Mn3+-Peak 5 | 56.21 | 1.2 | GL(20) | 0.04
11 | Mn2+-Peak 1 | 47.18 | 1.4 | GL(20) | 2.22
12 | Mn2+-Peak 2 | 47.8 | 1.59 | GL(20) | 0.71
13 | Mn2+-Peak 3 | 49.23 | 3.41 | GL(20) | 0.28
A
B
XPS spectra of Mn3p in α-MnO2 catalyst. The fitting parameters of the Mn3p spectra, such as the relative amounts of each oxidation state, were presented in (B). The spectra were fitted by considering Mn2+, Mn3+ and Mn4+ for Mn3p following the protocol created by Ilton, E.S. et al. (Ilton, E. S. et al., Appl. Surf. Sci. 2016, 366, 475.). The spectra were obtained using a pass energy of 23.5 eV and calibrated using the Au4f7/5 peak at 84.0 eV.

## Slide 2
Mn3p
24.77% Mn4+
70.02 % Mn3+
3.21% Mn2+
No | Name | Position (eV) | FWHM (eV) | Line shape | At%
1 | Mn4+-Peak 1 | 49.58 | 1.55 | GL(20) | 17.50
2 | Mn4+-Peak 2 | 50.93 | 1.55 | GL(20) | 4.52
3 | Mn4+-Peak 3 | 52.32 | 1.55 | GL(20) | 1.66
4 | Mn4+-Peak 4 | 53.72 | 1.55 | GL(20) | 0.91
5 | Mn4+-Peak 5 | 55.2 | 1.55 | GL(20) | 0.18
6 | Mn3+-Peak 1 | 48.38 | 1.4 | GL(20) | 40.99
7 | Mn3+-Peak 2 | 49.56 | 1.4 | GL(20) | 17.46
8 | Mn3+-Peak 3 | 50.75 | 1.4 | GL(20) | 9.55
9 | Mn3+-Peak 4 | 52.16 | 1.4 | GL(20) | 3.98
10 | Mn3+-Peak 5 | 56.21 | 1.2 | GL(20) | 0.04
11 | Mn2+-Peak 1 | 47.18 | 1.4 | GL(20) | 2.22
12 | Mn2+-Peak 2 | 47.8 | 1.59 | GL(20) | 0.71
13 | Mn2+-Peak 3 | 49.23 | 3.41 | GL(20) | 0.28
(A)
(B)
XPS spectra of Mn3p in α-MnO2 catalyst. The fitting parameters of the Mn3p spectra, such as the relative amounts of each oxidation state, were presented in (B). The spectra were fitted by considering Mn2+, Mn3+ and Mn4+ for Mn3p following the protocol created by Ilton, E.S. et al. (Ilton, E. S. et al., Appl. Surf. Sci. 2016, 366, 475.). The spectra were obtained using a pass energy of 23.5 eV and calibrated using the Au4f7/5 peak at 84.0 eV.

## Slide 3
Mn 3p
24.8% MnIV
72.0 % MnIII
3.2% MnII
(A)

## Slide 4
No | Name | Position (eV) | FWHM (eV) | Line shape | At%
1 | Mn4+-Peak 1 | 49.58 | 1.55 | GL(20) | 17.50
2 | Mn4+-Peak 2 | 50.93 | 1.55 | GL(20) | 4.52
3 | Mn4+-Peak 3 | 52.32 | 1.55 | GL(20) | 1.66
4 | Mn4+-Peak 4 | 53.72 | 1.55 | GL(20) | 0.91
5 | Mn4+-Peak 5 | 55.2 | 1.55 | GL(20) | 0.18
6 | Mn3+-Peak 1 | 48.38 | 1.4 | GL(20) | 40.99
7 | Mn3+-Peak 2 | 49.56 | 1.4 | GL(20) | 17.46
8 | Mn3+-Peak 3 | 50.75 | 1.4 | GL(20) | 9.55
9 | Mn3+-Peak 4 | 52.16 | 1.4 | GL(20) | 3.98
10 | Mn3+-Peak 5 | 56.21 | 1.2 | GL(20) | 0.04
11 | Mn2+-Peak 1 | 47.18 | 1.4 | GL(20) | 2.22
12 | Mn2+-Peak 2 | 47.8 | 1.59 | GL(20) | 0.71
13 | Mn2+-Peak 3 | 49.23 | 3.41 | GL(20) | 0.28